Bodyline 2k PU Plastic Adhesive Micro Emissions (ME)

Bodyline 2k PU Plastic Micro Emissions (ME) Adhesives are high-strength, structural adhesives that are resistant to exposure to elevated temperatures, moisture, *fuel, most solvents and chemicals. The adhesive systems are ideal for the universal repair and bonding of plastic bumpers, trim and vehicle components generally.

Free from Isocyanate o.1% = Removal of GHSO8 chest warning symbol from packaging.

H351 Phase removed

Contains no VOC.

GEV EC1 Certified for Low emissions.

Improved sanding over current.

Typical cure characteristics.

- Open Time @ 23°C      = 3min

- Handling time @ 23°C  =15min

- Sanding Time @ 23°C  =30min

- Optimum Bondline Thickness 0,5mm to 1,5mm

Features and benefits:

- Excellent specific adhesion to Polycarbonate, ABS, PVC, vehicle bumpers, trims and vehicle components generally.

- Super-Fast cure response at room temperature.

- Heat acceleration optional to achieve short cycle times. ( hand warm Max 36 Celsius)

- Free from Isocyanate o.1% Improved health and safety classification.

- Contains no VOC.

- GEV EC1 Certified for Low emissions.

- Improved sanding capabilities.

- Easy processing from cartridge.

- The 3min working time of the range. With an extended open time. The cure is complete enough for full handling in about 15 minutes.

- Bodyline Plastic Repair adhesives use a unique mixer tip, the smallest in the market reducing product waste.

- The bag in which these are packaged is an environmentally friendly sugar based zip bag.