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Bodyline 2k PU Plastic Adhesive Micro Emissions (ME)
 
Bodyline 2k PU Plastic Micro Emissions (ME) Adhesives are high-strength, structural adhesives that are resistant to exposure to elevated temperatures, moisture, *fuel, most solvents and chemicals. The adhesive systems are ideal for the universal repair and bonding of plastic bumpers, trim and vehicle components generally.

Free from Isocyanate o.1% = Removal of GHSO8 chest warning symbol from packaging. 
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H351 Phase removed 
[bookmark: _GoBack]Contains no VOC.
GEV EC1 Certified for Low emissions.
Improved sanding over current.


Typical cure characteristics.
· Open Time @ 23°C      = 3min
· Handling time @ 23°C  =15min 
· Sanding Time @ 23°C  =30min
· Optimum Bondline Thickness 0,5mm to 1,5mm 

Features and benefits: 
· Excellent specific adhesion to Polycarbonate, ABS, PVC, vehicle bumpers, trims and vehicle components generally. 
· Super-Fast cure response at room temperature.
· Heat acceleration optional to achieve short cycle times. ( hand warm Max 36 Celsius) 
· Free from Isocyanate o.1% Improved health and safety classification. 
· Contains no VOC.
· GEV EC1 Certified for Low emissions.
· Improved sanding capabilities.
· Easy processing from cartridge.
· The 3min working time of the range. With an extended open time. The cure is complete enough for full handling in about 15 minutes.
· Bodyline Plastic Repair adhesives use a unique mixer tip, the smallest in the market reducing product waste. 
· The bag in which these are packaged is an environmentally friendly sugar based zip bag. 
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